## Slide 1
Department of Mechanical & Aerospace Engineering, IIT Hyderabad
0
Finite Element Methods Lab
Elastic-Plastic Finite Element Analysis of Deep Drawing of a square cup
Dept. of Mechanical & Aerospace Engineering, IIT Hyderabad
Course Instructor: Dr. Muvvala Gopinath
BARATH.I
ME25MTECH11002

## Slide 2
Department of Mechanical & Aerospace Engineering, IIT Hyderabad
Finite Element Analysis of Deep Drawing of a square cup
1
Blank size: Sp= 124 mm, thickness t0= 1 mm
Punch size: Sp= 70 mm, punch profile radius: rpp= 8 mm, corner radius: rpc= 10 mm
Die size: Sd = 74 mm, profile radius: rdp= 5 mm, corner radius: rdc= 12 mm
For cold rolled steel σ = YS+K(ε)n MPa
Yield stress = 276 MPa, Strain Hardening exponent (n) : 0.8, Strength coefficient (K) ; 421 MPa
E = 210000 MPa, ν = 0.33
Coefficient of friction = 0.05

## Slide 3
PARTS
BLANK HOLDER
DIE
SHEET
PUNCH

## Slide 4
ASSEMBLY

## Slide 5
1) EFFECT OF PUNCH GEOMETRY ON THE ANALYSIS OF DRAWING
STRESS CONCENTRATION USING CIRCULAR PUNCH
STRESS CONCENTRATION USING SQUARE PUNCH
MAX VALUE :336.1 MPA
MAX VALUE :416.5MPA

## Slide 6
SPRING BACK EFFECT
DEFORMATION AT THE END OF PUNCHING
DEFORMATION AFTER RETRACTION OF PUNCH

## Slide 7
LOAD | MAXIMUM DEFORMATION | DEFORMATION AFTER PUNCH REMOVAL | SPRING BACK
5000 N | 15.06 | 14.6 | 0.46
10000 N | 15.02 | 14.7 | 0.32
15000 N | 14.9 | 14.6 | 0.3
20000 N | 15.02 | 14.69 | 0.33
Chart: VARIATION OF SPRING BACK
SB | 0.46 | 0.32 | 0.3 | 0.33

## Slide 8
Chart: VARIATION OF WRINKLE DEFECT
 | 0.105 | 0.102 | 0.091 | 0.092 | 0.077 | 0.062 | 0.038 | 0.024 | 0.012 | 0.001
STUDY ON WRINKLE DEFECT
1)BLANK HOLDING FORCE : 5KN
VARIATION ALONG PATH

## Slide 9
Chart: VARIATION OF WRINKLE
 | 0.09 | 0.086 | 0.083 | 0.075 | 0.063 | 0.044 | 0.03 | 0.018 | 0.008 | -0.001
2)BLANK HOLDING FORCE 10 KN
VARIATION ALONG PATH

## Slide 10
3)BLANK HOLDING FORCE 15 KN
Chart: VARIATION OF WRINKLE DEFECT
 | 0.106 | 0.101 | 0.094 | 0.089 | 0.077 | 0.062 | 0.039 | 0.024 | 0.012 | 0.001
VARIATION ALONG PATH

## Slide 11
4)BLANK HOLDING FORCE 20 KN
Chart: 
 | 0.098 | 0.095 | 0.085 | 0.083 | 0.066 | 0.054 | 0.035 | 0.02 | 0.009 | 0
Chart: 
 | 0.098 | 0.095 | 0.085 | 0.083 | 0.066 | 0.054 | 0.035 | 0.02 | 0.009 | 0
VARIATION ALONG PATH

## Slide 12
PUNCH LOAD WITH DISPLACEMENT
1)BLANK HOLDING FORCE 5KN
Chart: FORCE VS DISPLACEMENT
2)BLANK HOLDING FORCE 10KN
4)BLANK HOLDING FORCE 20KN
3)BLANK HOLDING FORCE 15KN